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A Gloss Silver metallic polyester (PET) specifically designed for use on ‘hot fuse’ Laser/Copier print systems. Some slight curl may occur on exiting the printer, but this will flatten quickly. This material is primarily used in the area of ‘long life’ durable, tracking or product labels, especially appliance & electronics labelling.

Face material properties 
Grammage



70 gsm + or – 6 gsm

Caliper (thickness)


55 microns + or – 5 microns

Adhesive

A clear permanent, acrylic based adhesive with good tack & adhesion on a wide range of surfaces. 

Minimum application temp.

+5(C

Storage range once applied

-20(C to +80(C

Backing

A one side clay coated, bleached kraft paper with good lay-flatness & stability

Thickness



88 microns + or – 5 microns

Grammage



90 gsm + or – 5 grams

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications but may vary. All products within our range are manufactured to BRC A + standards. The factory is also FSC and ISO14001 certified. Furthermore we are a Zero to landfill certified company. 

Market and Uses
Ideal for use on appliances and electronic equipment for safety warnings etc, a durable label with strong adhesive so difficult to remove, can also be used for PAT labels.  Good performance in damp conditions so again good for appliances that may get damp or be in storage.

Attention Grabbing Signs,  Electronics, Appliance labelss, PAT testing, Safety Signs etc etc.
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DATA SHEET:  Gloss Silver Metallic polyester with a permanent adhesive.  Short Code:  GSMP











Issue No 1: JR 16/6/2023











