A4 STOCK SPECIALITY SPEC SHEET

MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)
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White Paper Super Tack Adhesive







(ST)

Face material properties. 

A matt white, surface sized machine finished paper. This facestock is made from FSC™ Mix Credit certified pulp. Suitable for flexography, dot matrix, laser and ink jet. Printer settings may need to be adjusted for optimum print results.
Grammage



70 gsm

Caliper (thickness)


90 microns 

Adhesive

A very high tack rubber based “Hotmelt” adhesive. The initial tack is what sets this grade apart and with long term adhesion to match, it is a great problem solver, sticking well to rough, curved & non-polar surfaces! Recommended to be used in conjunction with our Window trim feature for medium and large volume applications.

Minimum application temp.

 -5°c
Storage range once applied
-40(C to + 50(C 
Backing

White siliconised Paper. Chosen to aid flatness and feeding characteristics.

Grammage



135gsm



Thickness



134microns

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications but may vary. All products within our range are manufactured to ISO 9001:2015 and BRC standards, the factory is also PEFC and FSC certified. The raw material laminates are also made to the same ISO standards as above and to ISO 14001.
2-year shelf life at 20-25 Deg c when stored in its original wrappings. 

*The face paper used for this grade has been manufactured as an FSC mix credit grade, however it is not supplied from our stock with this claim. 

Markets and Uses

Great for difficult to label surfaces that are rough or curved where a standard high tack will not work. Can be used on Hard Hats, smooth timber (roughly saw timber must be tested), corrugated metal surfaces, packaging that is flexible and possibly squashed as handled – ie pillow/quilts/wadding.
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