A4 STOCK SPECIALITY SPEC SHEET

MULTIPURPOSE (LASER/COPIER/INKJET PRODUCTS)
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White Paper Water Wash Off Adhesive.







(WW)

Face material properties. 

A bright white, surface –sized wood free paper with good opacity

Suitable for Most print methods. Including, Litho, all forms of dry toner, Ink-Jet Mono and various other digitally based over print systems. It will carry full colour print but is not suited to detailed work and should be assessed in detail before being used in such applications.

Grammage



71gsm

Caliper (thickness)


73 microns 

Adhesive

A good general-purpose permanent, acrylic based adhesive designed for water wash off applications. Best Wash Off results will be obtained with hot alkaline water but hot pure water or soapy water can also be used. FDA 21CFR 175.105 approved for Indirect food contact.  Water wash off performance can be affected by poor storage and any other ingress of moisture.
Minimum application temp.

 5(C

Storage range once applied
-20(C to +65(C (up to 200degC in short bursts when laser printing).
Backing

White siliconised Paper. Chosen to aid flatness and feeding characteristics.

Grammage



76gsm



Thickness



71 microns

Environmental

Paper components are either ECF or TCF grade manufactured using pulp from sustainable, managed resources. All dimensions are nominal target specifications but may vary. All products within our range are manufactured to ISO 9001:2015 and BRC standards, the factory is also PEFC and FSC certified. The raw material laminates are also made to the same ISO standards as above and to ISO 14001.
Shelf life is approx. 1 year when held at approx. 20-25deg c and in its original bags. 
Market and Uses
Ideal for use on products especially large plastic items, i.e. Indoor waste bins, storage boxes and trays where item is too big for outer packaging so directly labelled then washed off when/if required. Used in the brewery trade for labelling kegs which are then returned and re-used. Bottles and other solid containers that are re-cycled and re-used.

Breweries, Retail, Farm Shops, Cottage Industries, Plastic Item Manufacturers
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